## Slide 1
A fitted law for yield events, and everything rebuilt from it
Symbolic-regression discovery of the event-size distribution in AQS shear, the forward model built on it, and where the model fails
SEEM project status — September 4, 2026 (third pass; supersedes the August 6 deck)
AQS molecular-dynamics shear · 850 trajectories · nine preparations · 187,468 stress drops · every number regenerated by pipeline/run_all.sh

## Slide 2
The dataset, and the object of study
850
trajectories
9
cooling rates (256×)
187,468
stress-drop events
105,188
aging events
Protocol
Athermal quasistatic shear of a model glass; Δγ = 10⁻⁵, 49,999 steps per run, γ → 0.5
Cooling rates 2×10¹⁰ → 5.12×10¹² K/s in factor-of-2 steps, ~100 samples each
Per step: strain, stress, potential energy, cooling rate — nothing else is recorded
State and events
u = pe − u₀ (energy above the reference), τ = stress/10⁴
Stress drop: a step with dτ < 0, size s = −dτ; aging: du < 0 without a drop
22 × 22 grid on (u,τ): inner 20 × 20 on the 0.2–99.8% quantiles plus a catch-all ring
Takeaway — The target this time is the probability distribution of yield events, P(s | u,τ) — discovered, not assumed — and everything downstream is rebuilt from it.

## Slide 3
Framework: the step process as drift + jumps
Three fields measured directly, per cell
Elastic drift 2μ(u,τ), and the energy drift on quiet steps
Event hazard p(u,τ): fraction of steps that drop (median 0.32% per step)
Energy released per event: du = a + b·s + noise, per cell; an aging channel alongside
One law to discover
The size distribution P(s | u,τ): four decades of s, 187k events
First pass assumed a truncated power law (TPL); this pass asks the data for the form
Everything downstream — mean sizes, the plastic-rate field q, full synthetic stress–strain curves — is then derived from the fitted law and compared with its measured counterpart
Takeaway — Where derived and measured agree, the law carries the physics; where they disagree, we say so.

## Slide 4
Symbolic regression, built for scrutiny
Engine (library/symreg.py)
Exhaustive enumeration of expression trees: unary exp, log, 1/x, x², √x, −x; binary + − × ÷
Up to two constants fitted inside the nonlinearity (Levenberg–Marquardt, 4 restarts); outer affine profiled out
Numerical fingerprint dedup; hard admissibility (monotone decreasing); exact Pareto fronts
Complexity ≤ 8: 624,936 trees → ~14,000 distinct functions → ~10,300 admissible per cell
Protocol on the distributions
Target: binned ln ρ(s) per cell, 19 log bins, Poisson errors
12 cells (700–7,600 events) spanning the plane, plus unweighted-bin and wider-window variants
Audit: the largest cell pushed to complexity 9 — 4,505,024 trees, 48,725 admissible — no new form appears
SR proposes; the likelihood disposes (next slides)
Takeaway — Search the whole grammar, admit only monotone-decreasing densities, and let a per-event likelihood adjudicate among the Pareto knees.

## Slide 5
The discovered law, in one cell
The SR knee in the largest cells is log(1/(s+ε) − C), which rearranges to a bounded-support form:
P(s | u,τ) ∝ (s_c − s)ᵐ / (s + ε)ᵏ on 0 < s < s_c
k = 0.88: the small-event power law; ε = 2.8×10⁻⁵: rounds it off below the resolution
s_c(u,τ): a hard ceiling — the largest event the state can produce; the density vanishes like (s_c − s)ᵐ, m ≈ 2.3
The TPL’s exponential tail merely suppresses large events; the ceiling forbids them
Takeaway — Four decades of event size in one cell follow one four-parameter law whose only state-dependent parameter is the ceiling s_c.

## Slide 6
One shape everywhere; the fronts that found it
Left: twelve cells spanning 100× in scale collapse onto one curve in s/s_c with global (k, m, ε). Right: per-cell Pareto fronts (heights set by each cell’s own noise floor); orange, the complexity-9 audit run.
Takeaway — The state enters only through the ceiling: the shape is universal across the (u,τ) plane.

## Slide 7
SR proposes, the likelihood disposes
Normalized maximum likelihood per cell, seven families, AIC and trajectory-blocked cross-validation
The ceiling law wins 8 of 8 large cells: ΔAIC 67–120 over the TPL, 300–754 over the lognormal
A binned-least-squares favourite (√log form) was an artifact of Poisson weighting: ΔAIC ≈ +20,000 under likelihood
Synthetic control, both directions: TPL-generated catalogs return a TPL verdict 5/5; ceiling-generated return a ceiling verdict 5/5 with ε and s_c recovered to a few %
Sparse cells (< 1,000 events) cannot tell a ceiling from an exponential tail
Takeaway — The bounded-support law is decided by per-event likelihood with falsifiability controls, not by the binned fit.

## Slide 8
The ceiling field s_c(u,τ)
Left: 277 cells, 146× in range (0.02 cold → 3.0 in the flowing state), bootstrap error 6.5%; rank-1 factorization Λ(u)·f(τ) carries 95.5% of the log-variance. Right: refit by preparation at fixed cell — slow-cooled glass has a 1.71× higher ceiling than fast-cooled.
Takeaway — All state dependence, and all preparation memory, sit in one parameter — the ceiling.

## Slide 9
Rebuilding the plastic-rate field from the law
q = 1 − ⟨dτ⟩ / (2μ Δγ), measured per cell in the first pass
From the law: hazard × mean event size of the fitted distribution
Agreement: median +1.8%, RMS 17% against a 17.5% split-half noise floor — the test is saturated
The Λ(u)·f(τ) factors of the rebuilt field are the measured ones: f(τ) ∝ τ·log(1/τ − 0.44) vs 0.43; the Λ pole at u = 0.0287 vs 0.0280
Old κ ≈ 0.95 recovered as the mid-range slope; the x_min drift problem is gone with ε
Takeaway — The fitted law reproduces the first pass’s central object to within its noise floor.

## Slide 10
The acid test: simulating all 850 runs
Three arms differ only in the size law: ceiling law, TPL, empirical resampling. Stress–strain curves, yield overshoot across 256× in cooling rate, and flow stress (±5%) all emerge; yield-peak RMS 2.5% (ceiling), 1.4% (TPL), 0.9% (empirical).
Takeaway — The model predicts the yield strength of a glass from its preparation to a few percent — and macroscopic curves cannot tell size laws apart; the per-event likelihood can.

## Slide 11
The failure mode
The energy coordinate: good early, too convergent late
Preparations keep a 24% spread in mean u at γ = 0.5; the simulation keeps 4%
The fields are preparation-blind by construction (one map for all histories) — so this is the missing state variable of the first pass, seen macroscopically
Same message as the 1.71× ceiling memory: (u,τ) is not a sufficient state
Takeaway — A five-times-too-small preparation spread: the one place the two-variable model fails, and the question the rest of the deck answers.

## Slide 12
Where the preparation memory lives
Every channel re-measured per cooling rate at fixed cell; slope β on ln(rate) with cell fixed effects; a parity-split control gives the null
Event hazard: preparation-blind (β = −0.012 ± 0.002; ratio 1.005, control 1.02). Elastic drift: identical.
Mean event size: 1.70× (β = −0.117 ± 0.005) — the ceiling memory, measured another way; it lives in the tail (geometric mean moves only 1.20×)
A slow-cooled glass is triggered as often; its avalanches run further
73% of the per-event energy-release memory is size; 27% a secondary memory in the coupling
Takeaway — Memory acts through event size, not event rate — against the simplest one-variable STZ reading, where preparation enters through the STZ density.

## Slide 13
A one-parameter memory in the ceiling repairs the failure
Single change: s_c(u,τ; rate) = s_c(u,τ)·(rate/rate_mid)^β with the one global β = −0.117; hazard, drift, aging untouched
Spread of mean u at γ = 0.5: 4.1% → 26.5% against 24% in the data; the curve tracks the data over the whole strain window; yield peaks unchanged (2.5% → 2.8%)
Refinements overshoot (β by u-band: 37%; per-preparation coupling: 35%); the simple statement is the defensible one
Takeaway — To the resolution of this dataset, the missing state variable is a single multiplicative factor on the ceiling.

## Slide 14
The memory relaxes with strain
Nine-rate regression with a fixed effect per (cell, strain window): β = −0.21 → −0.11 → −0.05 → −0.04 from γ ≈ 0.15 to 0.45, and it falls within fixed u bands — relaxation, not state dependence; γ_r ≈ 0.18
Late strain: size memory 1.75× → 1.16×, hazard blind throughout; the energy-step memory only halves, a third of it in the coupling at fixed size
Whether that coupling memory also relaxes needs runs past γ = 0.5
Takeaway — The third variable is not a frozen label: plastic strain erases it on a scale of a few tenths — now measured, not assumed.

## Slide 15
The slow variable, one trajectory at a time
Parameter-free prediction: apply the between-preparation relation within a preparation — each trajectory gets exp(κ·δu₀) with κ = β·d ln(rate)/du₀ = −43
Predicted persistence of a sample’s initial energy deviation: 0.44 / 0.27 / 0.22 / 0.17 at γ = 0.1 / 0.2 / 0.3 / 0.5
Data: 0.63 / 0.27 / 0.24 / 0.18. Base model: 0.41 / 0.08 / 0.07 / 0.08. Tripling κ overshoots.
Same variable, same strength, acting on individual samples
Takeaway — A sample remembers its initial energy exactly as long as the preparation-level ceiling memory says it should.

## Slide 16
Is the ceiling just the largest event?
Refit with the top 1, 5, or 1% of events removed: s_c tracks the new maximum almost one-for-one (red)
So does a true ceiling with m ≈ 2 at n ≈ 5,000 (green synthetics: c/s_max 1.02–1.12)
A true TPL under the same fit runs off to 3–350× the maximum and collapses on refit (blue)
Merging consecutive drop steps into single avalanches (187k → 172k): the ceiling law wins by more (ΔAIC 117–213), s_c moves < 2%, k shifts +0.05
s_c in a cell is set by its ~10 largest events: the 6.5% bootstrap error is a floor
Takeaway — The data sit on the true-ceiling line, not the exponential cloud, and the law survives the event definition.

## Slide 17
Where the Markov assumption fails: aftershocks
At the same cell, the hazard on the step after an event is 20× the quiet baseline, decaying over ~5 steps; 14% of events sit in consecutive runs (Markov expectation 0.4%); the next event is 1.2× larger
Event counts per window are over-dispersed (Fano 1.3–1.6 vs the model’s 1.0) while the stress released per window is less variable (CV 0.10 vs 0.13)
Referenced to the last large event, the large-event hazard is 1.5× higher after 0.1–0.3 of reloading; large events are more regular (Fano 0.51 vs 0.71)
Takeaway — No function of (u,τ) produces this; an aftershock term fixes the yield peaks (RMS 2.5% → 1.6%) but not the variance below.

## Slide 18
The variance gap: ten exclusions, one open problem
Run-to-run scatter within a preparation: model 25–30% too high
Not the size law, aftershock hazard, grid (42×42), renewal hazard, two-class reload hazard
Not size–reload coupling (+0.02), size–size coupling (−0.01), relaxation rate (identical), the per-sample slow variable, or the u-channel noise terms
Each candidate was run forward and scored on the same three metrics (count Fano factor, CV of stress released per window, τ scatter)
What survives: a driving-noise amplitude 17% too large with the same restoring force, at fixed (u,τ), that no sequence correlation the data can exhibit accounts for
Closing it needs a per-step observable that is not (u,τ) — the same MD output the third variable asks for
Takeaway — The remaining discrepancy is bounded and named; the dataset has exhausted what it can test at fixed (u,τ).

## Slide 19
What holds, what doesn’t
SUPPORTED
One universal size shape with a single state-dependent scale (12 cells, 100× in scale)
A hard ceiling, sharper than exponential (8/8 by AIC; synthetic controls both ways; robust to merged avalanches)
Small-size exponent k ≈ 0.9; the ceiling field factorizes (95.5%)
Stress–strain curves and yield peaks across 256× in cooling rate at the few-% level
Memory in event size only; relaxes with γ_r ≈ 0.2; parameter-free per-sample prediction
NOT ESTABLISHED
Ceiling exponent m ≈ 2: order of magnitude only
Specific SR forms of the ceiling factors: best-of-front, not unique
Ceiling vs exponential in cells with < 1,000 events
Convergence of preparations at large strain — the model’s opinion, now with a measured rate but no data past γ = 0.5
The system size N (unrecorded): the finite-size reading of the ceiling is untested
CONTRADICTED
(u,τ) as a sufficient state — the 1.71× ceiling memory and the 5×-underpredicted u-spread, independently
The step process as Markov in (u,τ) at the 10⁻⁵ strain scale — aftershocks (×20), reload-dependent large events
Any of ten candidate explanations for the run-to-run variance excess
Preparation acting through the event rate (the simplest STZ-density reading)
Takeaway — The law and the model built on it hold at the few-percent level; their failures are located, quantified, and point at one slow variable and one non-Markov structure.

## Slide 20
Recommended next steps
1
A per-step structural observable from the MD
written alongside pe (local order, soft modes): the one test is whether it absorbs the ceiling’s β = −0.117 while leaving the hazard’s β at zero; it is also the last lever on the variance gap
2
Runs past γ = 0.5
one preparation to γ ≈ 2 settles whether the coupling memory relaxes like the ceiling memory, and whether preparations converge
3
System size N, ideally two sizes
the finite-size reading of the ceiling s_c stands or falls with it
4
Reverse loading
unchanged from the first pass — parity test for a back-stress variable
5
Interim model
the ceiling law with the one-parameter preparation memory and the aftershock hazard — the yield strength of a glass from its preparation history, to a few percent
Takeaway — Everything here is regenerated from the raw data by pipeline/run_all.sh (43 min); Figures 1–22 and the README carry the details.